ANNA UNIVERSITY, CHENNAI 25

### MODEL QUESTION PAPER

B.E. Aeronautical Engineering, VI SEMESTER

# AE343 COMPOSITE MATERIAL AND STRUCTURES

TIME – 3 Hours						MAXIMUM : 100 Marks

PART A                    		 (10 X 2 = 20 Marks)

ANSWER ALL QUESTIONS

1.	What are the advantages of composites?

2.	Explain difference between fibers and whiskers?

3.	Name any four aircraft using composites and parts in which used.

4.	What are natural axes?

5.	What are the assumptions made in netting analysis?

(The basic assumption in netting analysis is fibers provide)

6.	What is meant by failure envelope?

7.	Explain the function and desirable properties of resins used in FRP.

- For a composite Ef = 100 Gpa, Em 10 Gpa. Calculate the percentage increase

in load carrying capacity of a uniaxial bar when the fibre increased from 70 to 80%.

9.	What is the difference between open mould and closed mould process?

10.	Explain sandwich construction. Give example for face and core material.

PART B                    		 (5 X 16 = 80 Marks)

11.		Determine E1 & E2 for lamina using macro - mechanics where 1 and 2 are

arbitrary axis									(16)

12 (a)		Using machines of material approach obtain expressions for E1, E2, G12 , 12 and

show their relations with Vf  							(16)

( OR )

(b)		In a built up aluminium alloy I-section shown in fig.1. One flange was removed

and replaced by steel angle of same dimensions. Calculate the change in rivet

shear for a shear load of 10000N. The rivets have 4mm diameter and 20mm

spacing. EAl = 70 Gpa.							(16)

All dimensions in mm

Figure 1

13 (a)		Derive the governing differential equation for an unidirectional anistropic plate

and reduce if  to orthotropic plates and isotropic plates.			(16)

( OR )

(b)		List down the boundary conditions used for the analysis of laminated plate (both

simply supported and fixed edges) obtain the expression for the maximum

deflection of a simply supported orthotropic plate subjected to uniformly

distributed load of intensity qo.							(16)

14 (a)		For the following laminate configuration compute the stiffness matrices. No of

layers 4, Each layer is 1mm thickness 0 / - 45 / 45 / 90.

E1 = 40 Gpa, E2 = 8 Gpa G12 > 4 Gpa. γ12 = 0.25 				(16)

( OR )

- A composite laminate has 3 layers with fibre orientation 0 / 90 / 0. Top layer

an bottom layer thickness is 2mm (each and middle layer thickness is 3 mm.

Given Nx = 50 N/m,       Ny = 200 N/m Nxy = 300 N/m Mx = 1000N, My = 1000

N & Mxy = 500N compute the strain and curvature. E1 = 180 Gpa, E2 = 15 Gpa,

G12 = 7 Gpa, γ12 = 0.28. 							(16)

15 (a)		Describe any two methods for production of fibers				(16)

( OR )

- Explain any two methods, one under open mould process and one under closed

mould process.									(16)